## Slide 1: Microscopic Methods for Chemists – with an emphasis on SEM
Charge Transfer Processes in Hydrodynamic systems
Martin Jönsson-Niedziółka martinj@ichf.edu.pl Bluesky: @jonsson-niedziolka.pl

## Slide 2: Practical Information
7 lectures
4-hour practical (groups of 3)
Exam: Measure “mystery sample”
Analyse images (size, composition)
Hand in report
Info on www.charge-transfer.pl/sem-course
Content
How everything started…basics and background
Optical microscopy towards nanoscopy
Scanning probe microscopy
Electron microscopy – principles, electron-material interaction
What affects SEM and how to obtain good a good image
SEM vs. TEM
EDX
Our system & practical notes
Practical SEM session (4h)

## Slide 3
1 µm
500 nm
50 nm
5 nm
1 nm
0.5 nm
0.1 nm
5 µm
  Widefield
  Stereo
  Confocal
  Superresolution
  Scanning Electron
  Transmission Electron
  Scanning He-Ion
  Focused Ion Beam
Optical and SEM micrograph of the
radiolarian Trochodiscus longispinus
Electron Micrograph
Optical Micrograph
Overview

## Slide 4
First Pioneers of Microscopy
1670s

## Slide 5
1850s
first microscopes
1860s
theory of microscopy
1880s
Optical-grade glass
1890s
Optimised illumination
First Pioneers of Microscopy

## Slide 6
Nature of Microscopy
Optics
Ray – Waves - Particles
(geometrical optics) (physical optics)
Reflection
Refraction
Diffraction
Interference
Polarisation

## Slide 7
Nature of Microscopy
Optics
Ray
(geometrical optics)
Reflection
Refraction
nd,F,C = refractive index of the material for wavelengths 587.56 nm, 656.3 nm, 486.1 nm
glass ≠ glass

## Slide 8
Nature of Microscopy
Optics
Ray – Waves - Particles
(geometrical optics) (physical optics)
Diffraction
Interference
Polarisation
More on this later…

## Slide 9
Abbe said:
“The microscope image is an interference effect of a diffraction phenomenon.”
And Richard Feynman said:
“No-one has ever been able to define the difference between interference and diffraction satisfactorily. It is just a question of usage, and there is no specific, important physical difference between them. The best we can do, roughly speaking, is to say that when there are only a few sources, say two, interfering, then the result is usually called interference, but if there is a large number of them, it seems that the word diffraction is more often used.”

## Slide 10
Polarizers
Reflective polarizers, e.g. parallel wire grid polarizers (parallel light is reflected, while perpendicular polarized light is transmitted).
Dichroic polarizers e.g nanoparticle polarizers (absorb a specific polarization of light).
Birefringent polarizers (filtered by different refractive index of the polarization of light).
Unpolarized light rapidly varying random combination of p- and s-polarized light.
Ideal linear polarizer I=I/2 (just p- or s-polarized light)
Polarisation
Tiny crystallites of iodoquinine sulfate, oriented in the same direction, are embedded in a transparent polymeric film to prevent migration and reorientation of the crystals. Land developed sheets containing polarizing films that were marketed under the trade name of Polaroid®, which has become the accepted generic term for these sheets.
Birefringent materials are optically anisotropic and the refractive index of such materials depends on the direction in which light propagates through it. Birefringence means a ray of unpolarized light is divided into two rays by refraction when passing through the material. Birefringent materials have a highly ordered molecular structure.
Malus’ law describes transmitted intensity I by
I=I0cos2θ
With
θ = angle between the incident linear polarization and the polarization axis
I0 = intensity of linear polarized light

## Slide 11
The resolution r of small structures is limited due to light diffraction in relation to the wavelength .
Abbe equations
The magnification of an object is achieved by the arrangement of several lenses with different refractive indices and geometries.
Numerical Aperture (NA):
with half of the objective’s opening angle () and the refractive index ().
magnification ≠ resolution
2D → Airy disc
3D → point-spread function

## Slide 12
Fourier optics to describe coherent image formation, imaging obtained by illuminating the specimen with spatially coherent light.
with:
Magnification
U3 is the Fourier-transformed representation of U2, which is that of U1!
This ratio can be made arbitrarily large!

## Slide 13
The resolution r of small structures is limited due to light diffraction in relation to the wavelength .
Abbe equations
The magnification of an object is achieved by the arrangement of several lenses with different refractive indices and geometries.
Numerical Aperture (NA):
with half of the objective’s opening angle () and the refractive index ().
magnification ≠ resolution
2D → Airy disc
3D → point-spread function

## Slide 14
Contact:
Martin Jönsson-Niedziółka
email: martinj@ichf.edu.pl
Bluesky: @jonsson-niedziolka.pl